## Slide 1
Imported Coal QA

## Slide 2
Imported Value Chain – Material Flow

## Slide 3
Variation of Ash% reported at different nodes vs Load Port April’23- March’24
As we move from Load Port to plant the variation in the reported value of Ash% increases – This reflects the capability of measurement system owing to factors such as natural variation because of heterogeneity of coal, Vessel level vs rake level analysis, measurement methods
Reported values are generally on lower side at TSJ and on higher side at TSK.
LP: Load Port | DP: Discharge Port | POR – Port Outgoing Rake | PIR – Plant Incoming Rake

## Slide 4
As we move from Load Port to plant the variation in the reported value of VM% increases for the same reason as ash.
Reported values are generally on higher side at TSJ having high variation w.r.t LP report.
LP: Load Port | DP: Discharge Port | POR – Port Outgoing Rake | PIR – Plant Incoming Rake
Variation of VM% reported at different nodes vs Load Port April’23- March’24
Diff in VM% reporting

## Slide 5
Current State
Study for determination of tolerance in reported coal ash
As per the analysis done with external agency, current tolerance has been taken for Ash as 0.28, which only accounts for variations due to inter-lab testing.
R&R tolerance = = = 0.48 units
Proposed State
As suggested in IS- 1350
+/- 0.48 as per R&R tolerance mentioned in the standard
As per SABS CRM -023, testing done in FY20
As suggested in IS- 16143
+/- 0.55 at TSJ
Parameters | Description | TSJ
V1 | Primary Increment Variance | 3
VPT | Preparation and testing variance | 0.2
n | No of increments per sub lots | 12
m | No of sublots in the lot | 6
PL | Overall precision of sampling , sample preparation and testing for the lot | 0.55
Case A: As per IS-1350 (Old standard)
Case B: As per IS-16143 (New standard)

## Slide 6
The IS 16143 prescribes how to design our process to achieve any required precision.
Basis our current process design, we have calculated the precision/tolerance value.
The Sc.Serv team has done the flight sample variation study across TSL labs and had submitted their findings in report attached.
The report shows the actual VPT value based on different coal grades basis Ash & VM range.
The +/- 0.55 value was recalibrated for different coal grades in next slides.
As suggested in IS- 16143
+/- 0.55 at TSJ
Parameters | Description | TSJ | EXP
V1 | Primary Increment Variance | 3 | 3
VPT | Preparation and testing variance | 0.2 | 0.1
n | No of increments per sub lots | 12 | 20
m | No of sublots in the lot | 6 | 8
PL | Overall precision of sampling , sample preparation and testing for the lot | 0.55 | 0.35
Case B: As per IS-16143
Study for determination of tolerance in reported coal ash - Backup
Precision
(*PL)
Primary increment variance(V1)
Preparation & testing variance(VPT)
No of sublots in a lot (m)
No of increments per sublots (n)
*To improve the precision
Standardization of sample collection, preparation and testing methods is to be done
Case 3: If we reduce the *VPT from 0.2 0.10 the tolerance can be reduced to +/-0.48
Case:2 If we increasing the *no of sublot to 8’m value’ keeping VPT at 0.2, the tolerance can be reduced to +/-0.48
Case:1 If Increasing the *no of increments per sublots from 12 to 20 the tolerance can be reduced to +/-0.48 keeping others constant
Aspirational target

## Slide 7
Grade wise tolerance on the basis of Ash & VM range wise |  |  | VM Range |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  | Min | 13 |  | 16 |  | 19 |  | 22 |  | 25 |  | 28 |  | 31 |  | 34 | 
 |  |  | Max | 16 |  | 19 |  | 22 |  | 25 |  | 28 |  | 31 |  | 34 |  | 37 | 
 | Min | Max |  | EL |  | VL |  | L |  | LM |  | HM |  | H |  | VH |  | EH | 
Ash Range | 2.37 | 5.5 | VL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 5.5 | 13 | L | Jellinbah PCI JLV PCI SW PCI |  | Bedford |  | Daunia Bedford |  | Byerween Goonyella Poitrel |  | Australian HCC |  |  |  | Kestral |  | Indo SMM | 
 |  |  |  | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM
 |  |  |  | 0.29 | 0.65 | 0.17 | 0.58 | 0.44 | 0.64 | 0.32 | 0.58 | 0.25 | 0.52 |  |  | 0.24 | 0.6 | 0.44 | 0.65
 |  |  |  | 0.29 | 1.16 | 0.2 | 1.3 | 0.27 | 0.78 | 0.12 | 0.39 | 0.7 | 1 |  |  | 0.21 | 2 | 0.16 | 2.2
 | 13 | 18 | M |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 18 | 22.5 | H |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 22.5 | 24.3 | VH |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Analysis for different grades of Coal by Sc.Serv- Flight sample Interlab Tolerance of Ash & VM w.r.t CRM value
CRM tested value
Tolerance ≤Assigned CRM value
Tolerance>Assigned CRM Value
The above table shows the flight sample preparation and testing done across TSJ,TSK & TSM labs for different coal grades.
The Ash & VM flight sample tolerance limit was proposed by scientific services team as compared to CRM tested value
The above table is showing the VPT value which was taken as 0.2 earlier for calculation of the tolerance limit.
New tolerance as per actual VPT is calculated for all the available coal grades data
Parameters | Description | TSJ
V1 | Primary Increment Variance | 3
VPT | Preparation and testing variance | 0.2
n | No of increments per sub lots | 12
m | No of sublots in the lot | 6
PL | Overall precision of sampling , sample preparation and testing for the lot | 0.55
As per IS-16143

## Slide 8
Ash tolerance for flight sample varies in range Min-0.17 to Max- 0.44
Ash tolerance for plant sites varies in range Min-0.53 to Max- 0.68
VM tolerance for flight sample varies in range Min-0.52 to Max- 0.65
VM tolerance for plant sites varies in range Min-0.72 to Max- 0.77
Coal Grade wise tolerance based on Ash & VM range wise |  |  | VM Range |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  | Min | 13 |  | 16 |  | 19 |  | 22 |  | 25 |  | 28 |  | 31 |  | 34 | 
 |  |  | Max | 16 |  | 19 |  | 22 |  | 25 |  | 28 |  | 31 |  | 34 |  | 37 | 
 | Min | Max |  | EL |  | VL |  | L |  | LM |  | HM |  | H |  | VH |  | EH | 
Ash Range | 2.37 | 5.5 | VL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 5.5 | 13 | L | Jellinbah PCI JLV PCI SW PCI Blended PCI NEBO PCI Jellinbah + LV PCI SW PCI |  | Bedford Capricon PCI CURRAGH+BARALABA PCI BLEND INDONESIAN PCI Q Coal PCI (WEAK) Saraji CC Trident |  | Daunia Bedford 10.5% ASH BHP OHCC BC7 BURTON_HCC Daunia LV HCC LV PCI MANUCODE PMV PDN PCI CD HCC Morabah North |  | Byerween Goonyella Poitrel 11.7% ASH BHP OHCC BROLGA CONUMA HCC Illawara IP EAST LV PCI (WEAK) MetRes HCC Millenium HCC POITREL PCI (23% VM) WEAK Teck Standard Teck Standard (OHCC) WHYALLA PCI Ammonate Byerwen Caval ridge Goonyella Poitrel Soft RIVERSIDE |  | Australian HCC Illawara TAHMOOR BWW |  | DAWSON MET COAL Sonoma |  | Kestral BLUEWATER SS CME HVA CME SOFT JULIET Nantoy Kestrel Falcon SS |  | Indo SMM SMM WENTZ | 
 |  |  |  | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM | Ash | VM
 |  |  |  | 0.29 | 1.16 | 0.2 | 1.3 | 0.27 | 0.78 | 0.12 | 0.39 | 0.7 | 1 |  |  | 0.21 | 2 | 0.2 | 2.2
 |  |  |  | 0.29 | 0.65 | 0.17 | 0.58 | 0.44 | 0.64 | 0.32 | 0.58 | 0.25 | 0.52 |  |  | 0.24 | 0.6 | 0.44 | 0.65
 |  |  |  | 0.60 | 0.77 | 0.53 | 0.74 | 0.68 | 0.77 | 0.62 | 0.74 | 0.58 | 0.72 |  |  | 0.57 | 0.75 | 0.68 | 0.77
 | 13 | 18 | M |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 18 | 22.5 | H |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 22.5 | 24.3 | VH |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Tol for Flight sample
Tol for plant sites
CRM tested value
Ash & VM tolerance calculated for different grades of Coal

## Slide 9
Comparison study of Imported Coal Ash tolerance- For Jellinbah PCI reported ash March’23-April’24
Case B: Comparison of deviations with current & proposed tolerance
TSJ
TSK
TSM
No of Rakes-18
No of Rakes-28
No of Rakes-57
With Current tolerance limit 0.28
With proposed tolerance limit 0.55
No of Rakes outside limit -8
No of Rakes outside limit -7
No of Rakes outside limit -49
No of Rakes outside limit -5
No of Rakes outside limit -3
No of Rakes outside limit -28
% Rakes outside limit -45%
% Rakes outside limit -25%
% Rakes outside limit -86%
% Rakes outside limit -28%
% Rakes outside limit -11%
% Rakes outside limit -49%
Total No of Rakes-103 for Jellinbah PCI in FY24
Comparison study of single coal grade reported ash% - LP reported value vs at plant sites.
103 Rakes of Jellinbah PCI were received from March’23 to April’24( IRQA).
No of deviation with existing tolerance set point & proposed set point were compared to quantify the impact on deviation %
For Jellibah PCI (Sample case) ~50% deviation in the system is due to type I error.
LP reported ash%
Plant sites reported ash%
Type of errors – Type I & Type II errors

## Slide 10
Grade | Basket | No of Rakes | At +-0.28 Cut off |  |  |  | At +-0.55 Cut off |  |  |  | Rakes outside+-0.28 | Rakes outside+-0.55 | Cumulative at 0.28 | Cumulative at 0.55
 |  |  | TSJ | TSK | TSM | HMC | TSJ | TSK | TSM | HMC |  |  |  | 
BEDFORD | OHCC | 173 | 60% |  |  | 65% | 38% |  |  | 35% | 105 | 62 | 61% | 36%
GOONYELLA | PHCC | 96 | 57% | 77% | 68% |  | 43% | 50% | 41% |  | 66 | 41 | 69% | 43%
Poitrel soft | SS | 114 | 72% |  | 73% | 40% | 39% |  | 32% | 15% | 77 | 32 | 68% | 28%
SMM | SS | 126 |  | 91% | 54% |  |  | 63% | 22% |  | 80 | 41 | 63% | 33%
JELLINBAH PCI | PCI | 103 | 45% | 25% | 86% |  | 28% | 11% | 49% |  | 64 | 36 | 62% | 35%
 | Total Rakes | 612 |  |  |  |  |  |  |  |  | 392 | 212 | 64% | 35%
The 5 coal grades have maximum data points available in last one year, selection of these grades done basis
  Representation of each basket
  Highest volume in the bucket.
At our proposed tolerance of +/-0.55 noise in the system gets reduced by 30%.
Case B: Comparison of deviations with current & proposed set point for different grades of coal
Comparison study of Imported Coal Ash tolerance- For other grades of coal March’23-April’24

## Slide 11
Control chart for all grades difference in reporting at plant sites vs LP ash%
TSJ - 103 rakes; Oct-23 to Dec-23
TSJ - 144 rakes; Feb-24 to May-24
From Feb’24 onwards the sample preparation process was mechanized at TSJ which shows the bias in ash analysis has been reduced.
Earlier process
After Implementing mechanized process for coal crushing

## Slide 12
Control chart for Jellinbah PCI difference in reporting at TSM vs LP ash%- March’23-April’24
TSM- 57 rakes
+0.55
-0.55
+0.28
-0.28
Values above+/- 0.55 area the assignable causes

## Slide 13
Method of Reporting Ash% - Jellinbah PCI reported ash% comparison study March’23-April’24
Chart: 
LP(ADB)
All Plant site(DB)
Chart: 
LP(DB)
All Plant site(DB)
Location | Method | Ash%
LP | Air Dry basis | 10.33
LP | Dry basis | 10.44
Plant sites | Dry basis | 10.67
Currently LP is reporting in ‘Air dry basis’ (ADB) which is lower than ‘Dry basis’ (DB) by a factor of= ( )~ 1.01
TSJ
TSK
TSM
Dry basis= ( )* Air dry basis which will be on a higher side.

## Slide 14
IRQA
If Difference exceeds 0.55 w.r.t LP complaint to be logged against responsible stakeholder
LP | DP | POR | PIR | DP-LP | POR-LP | PIR-LP` | Example Case
7.40 | 7.65 | 7.78 | 6.87 | 0.25 | 0.38 | 0.53 | 

## Slide 15
Complaint Matrix
Support Functions : Strategic Procurement/RM Planning/Sc. Ser./PTG
Coal Supplier + Strategic Procurement
Port Operations
Rail Logistics
RMM
Coke Plant Operation
Supplier | Supplier | Port Operations | Port operation | Rail logistics | RMM | RMM |  | 
 | LP | DP | Port Outgoing Rake |  | Plant Incoming Rake |  | Responsible Stakeholder | Probable cause
Scenario-01 | 10 | 10.6 (Diff-0.6) NC | 10.4 (Diff-0.6) C |  | 10.4 (Diff-0.4) C |  | Port Operations | Mix-up during transit or at port, wrong Testing & Measurements
Scenario-02 | 10 | 10.3 (Diff-0.3) C | 10.6 (Diff-0.6) NC |  | 10.4 (Diff-0.4) C |  | Port Operations | Mix-up at port, wrong Testing & Measurements
Scenario-03 | 10 | 10.3 (Diff-0.3) C | 10.4 (Diff-0.4) C |  | 10.6 (Diff-0.6) NC |  | Rail logistics & Scientific Services | Mix-up during transit by rail logistics, wrong Testing & Measurements at plant sites
Scenario-04 | 10 | 10.6 (Diff-0.6) NC | 10.8 (Diff-0.8) NC |  | 10.4 (Diff-0.4) C |  | Port Operations | Mix up at port or wrong Testing & Measurements
Scenario-05 | 10 | 10.6 (Diff-0.6) NC | 10.4 (Diff-0.4) C |  | 10.6 (Diff-0.6) NC |  | Port Operations & Rail logistics | Mix-up during transit or at port, wrong Testing & Measurements
Scenario-06 | 10 | 10.4 (Diff-0.4) C | 10.6 (Diff-0.6) NC |  | 10.8 (Diff-0.8) NC |  | Port operations & Rail logistics | Mix-up during transit or at port, wrong Testing & Measurements
Scenario-07 | 10 | 10.3 (Diff-0.3) C | 10.4 (Diff-0.4) C |  | 10.5 (Diff-0.5) C |  | No Complaint | No Complaint
Scenario-08 | 10 | 10.6 (Diff-0.6) NC | 10.6 (Diff-0.6) NC |  | 10.6 (Diff-0.6) NC |  | Coal supplier | Wrong Material supplied

## Slide 16
From feb onwards the sample preparation process was mechanized at TSJ
From feb onwards, At CRMT lab, Jamshedpur mechanized means was introduced during sample preparation and results of Ash % reporting has improved as compared to the previous reported values.
Last 6 months comparison study done for LP ash reported vs Rake level reported values.
Box plot of Ash% rake Analysis – LP vs Plant site for all grades of coal as per IRQA Oct’23-Mar’24
Month wise | Count of TSJ Samples
OCT | 38
NOV | 30
DEC | 36
JAN | 11
FEB | 31
MAR | 34
Grand Total | 180

## Slide 17
Month | Count of TSJ Samples
Nov'23 | 68
Dec'23 | 96
Jan'24 | 99
Feb'24 | 99
Mar'24 | 94
Apr'24 | 91
May'24 | 58
Grand Total | 605
From feb onwards, At CRMT lab, Jamshedpur mechanized means was introduced during sample preparation and results of Ash % reporting has improved as compared to the previous reported values.
Last 7 months comparison study done for LP VM reported vs Rake level reported values.
From feb onwards the sample preparation process was mechanized at TSJ
Box plot of VM % rake Analysis – LP vs plant site for all grades of coal as per IRQA Nov’23-May’24

## Slide 18
Thank You

## Slide 19
The IS 16143 prescribes how to design our process to achieve any required precision.
Basis our current process design, we have calculated the precision/tolerance value.
The calculated precision value (+/- 0.55) is based on our initial assumption of VPT taken as 0.2 (As suggested in IS standard if initial value is not available)
The Sc.Serv team has done the flight sample variation study across TSL labs and had submitted their findings in report attached.
The report shows the actual VPT value based on different coal grades basis Ash & VM range.
The +/- 0.55 value was recalibrated for different coal grades in next slides.
As suggested in IS- 16143
+/- 0.55 at TSJ
Parameters | Description | TSJ | EXP
V1 | Primary Increment Variance | 3 | 3
VPT | Preparation and testing variance | 0.2 | 0.1
n | No of increments per sub lots | 12 | 20
m | No of sublots in the lot | 6 | 8
PL | Overall precision of sampling , sample preparation and testing for the lot | 0.55 | 0.35
Case B: As per IS-16143
Study for determination of tolerance in reported coal ash - Backup
Precision
(*PL)
Primary increment variance(V1)
Preparation & testing variance(VPT)
No of sublots in a lot (m)
No of increments per sublots (n)
*To improve the precision
Standardization of sample collection, preparation and testing methods is to be done
Case 3: If we reduce the *VPT from 0.2 0.10 the tolerance can be reduced to +/-0.48
Case:2 If we increasing the *no of sublot to 8’m value’ keeping VPT at 0.2, the tolerance can be reduced to +/-0.48
Case:1 If Increasing the *no of increments per sublots from 12 to 20 the tolerance can be reduced to +/-0.48 keeping others constant
Aspirational target

## Slide 20
Domestic coal - reported ash% comparison study WB vs plant sites - Feb’23-April’23
Domestic Coal-Comparison of deviations with current & proposed set point
TSJ
TSK
TSM
No of Rakes-81
No of Rakes-41
No of Rakes-59
With Current tolerance limit 0.28
With proposed tolerance limit 0.55
No of Rakes outside limit -80
No of Rakes outside limit -21
No of Rakes outside limit -37
No of Rakes outside limit -77
No of Rakes outside limit -6
No of Rakes outside limit -21
% Rakes outside limit -99%
% Rakes outside limit -51%
% Rakes outside limit -63%
% Rakes outside limit -95%
% Rakes outside limit -15%
% Rakes outside limit -36%
Total No of Rakes-181 domestic coal rake supplied to plant sites
West Bokaro reported ash%
Plant sites reported ash%
The Domestic coal supplied to plant sites also shows the sample implication as seen in imported coal.
At our proposed tolerance of +/-0.55 noise in the system gets reduced by 30%.
WB

## Slide 21
SAMPLE COLLECTION AND PREPARATION
10 Kgs of flight sample is collected as per ASTM standard and dispatched though courier services to CRMT lab.
The flight sample is 1st passed through the -12.5mm sieve and oversize samples are crushed mechanically (Earlier Manual means was used) using jaw crusher till all the samples passes through, followed by coning and quartering till sample is reduced to 2-2.5 kgs.
The reduced 2-2.5 kgs is then crushed to -3.35 mm using jaw crusher and is passed through -3 mm sieve followed by Coning and quartering till sample is reduced to 0.2-0.25 kgs.
Reduced sample of 0.2-0.25 kgs, sample is kept in hot air oven for 1 hr at 105 deg. Celsius for removing the moisture.
OBSERVATION
TSJ
Before
After
Sample Preparation of Imported Coal

## Slide 22
Control chart for all grades difference in reporting at plant sites vs LP ash%
TSK - 305 rakes; Apr-23 to May-24
In TSK it is observed when LP reporting is changed from ABD DB the values will come closer to reported values

## Slide 23
Jellinbah PCI reported ash% comparison study w.r.t reporting method March’23-April’24
Chart: 
 | 10 | 10.9 | 10.6 | 10.6 | 10 | 10.5 | 10 | 10.6 | 10 | 10.5 | 10.2 | 10.5 | 10 | 10 | 10.6 | 10 | 10.5
 | 10.55 | 11.45 | 11.15 | 11.15 | 10.55 | 11.05 | 10.55 | 11.15 | 10.55 | 11.05 | 10.75 | 11.05 | 10.55 | 10.55 | 11.15 | 10.55 | 11.05
 | 9.45 | 10.35 | 10.05 | 10.05 | 9.45 | 9.95 | 9.45 | 10.05 | 9.45 | 9.95 | 9.65 | 9.95 | 9.45 | 9.45 | 10.05 | 9.45 | 9.95
 | 10.11 | 9.96 | 10.41 | 10.41 | 11.04 | 10 | 10.21 | 10.59 | 10.23 | 10.29 | 10.59 | 10.27 | 10 | 10.8 | 11.68 | 10.02 | 10.18
TS02TWS120
TS03TWS65
T01NHT31
K03TWS19
TS02TWS108
K02TWS13
TS02TWS91
K03TWS24
TS02TWS97
TS03TWS74
T08NHT59
K03TWS10
TS02TWS112
TS02TWS104
K03TWS22
TS02TWS116
TS03TWS65
Chart: 
 | 10.1 | 11.009 | 10.706 | 10.706 | 10.1 | 10.605 | 10.1 | 10.706 | 10.1 | 10.605 | 10.302 | 10.605 | 10.1 | 10.1 | 10.706 | 10.1 | 10.605
 | 10.65 | 11.559 | 11.256 | 11.256 | 10.65 | 11.155 | 10.65 | 11.256 | 10.65 | 11.155 | 10.852 | 11.155 | 10.65 | 10.65 | 11.256 | 10.65 | 11.155
 | 9.55 | 10.459 | 10.156 | 10.156 | 9.55 | 10.055 | 9.55 | 10.156 | 9.55 | 10.055 | 9.752 | 10.055 | 9.55 | 9.55 | 10.156 | 9.55 | 10.055
 | 10.11 | 9.96 | 10.41 | 10.41 | 11.04 | 10 | 10.21 | 10.59 | 10.23 | 10.29 | 10.59 | 10.27 | 10 | 10.8 | 11.68 | 10.02 | 10.18
TS02TWS120
TS03TWS65
T01NHT31
K03TWS19
TS02TWS108
K02TWS13
TS02TWS91
K03TWS24
TS02TWS97
TS03TWS74
T08NHT59
K03TWS10
TS02TWS112
TS02TWS104
K03TWS22
TS02TWS116
TS03TWS65
LP(ADB)
LP(ADB)+0.55
LP(ADB)-0.55
TSJ(DB)
LP(DB)
LP(DB)+0.55
LP(DB)-0.55
TSJ(DB)
Location | Method | Ash%
LP | Air Dry basis | 10.32
LP | Dry basis | 10.42
TSJ | Dry basis | 10.28
Air Dry (ADB) at LP to Dry Basis (DB) at TSJ
Dry basis (DB) at LP to Dry Basis (DB) at TSJ

## Slide 24
Jellinbah PCI reported ash% comparison study w.r.t reporting method March’23-April’24
Chart: 
 | 10.2 | 10.4 | 10.1 | 10.4 | 10.6 | 10.3 | 10.3 | 10.3 | 10.2 | 10.3 | 10.2 | 10.2 | 10.5 | 10.6 | 10.6 | 10.9 | 10.5 | 10.6 | 10.5 | 10.5 | 10.1 | 10.2 | 10.9 | 10.5 | 10.2 | 10.4 | 10.3 | 10.5
 | 9.84 | 9.56 | 10.49 | 10.82 | 10.78 | 9.9 | 10.84 | 10.45 | 10.78 | 9.71 | 10.25 | 11.34 | 9.89 | 10.51 | 10.33 | 11.12 | 10.17 | 10.51 | 10.51 | 10.13 | 10.76 | 10.58 | 11.07 | 10.42 | 10.6 | 10.41 | 10.77 | 10.31
 | 10.75 | 10.95 | 10.65 | 10.95 | 11.15 | 10.85 | 10.85 | 10.85 | 10.75 | 10.85 | 10.75 | 10.75 | 11.05 | 11.15 | 11.15 | 11.45 | 11.05 | 11.15 | 11.05 | 11.05 | 10.65 | 10.75 | 11.45 | 11.05 | 10.75 | 10.95 | 10.85 | 11.05
 | 9.65 | 9.85 | 9.55 | 9.85 | 10.05 | 9.75 | 9.75 | 9.75 | 9.65 | 9.75 | 9.65 | 9.65 | 9.95 | 10.05 | 10.05 | 10.35 | 9.95 | 10.05 | 9.95 | 9.95 | 9.55 | 9.65 | 10.35 | 9.95 | 9.65 | 9.85 | 9.75 | 9.95
10.10
Chart: 
 | 10.302 | 10.504 | 10.201 | 10.504 | 10.706 | 10.403 | 10.403 | 10.403 | 10.302 | 10.403 | 10.302 | 10.302 | 10.605 | 10.706 | 10.706 | 11.009 | 10.605 | 10.706 | 10.605 | 10.605 | 10.201 | 10.302 | 11.009 | 10.605 | 10.302 | 10.504 | 10.403 | 10.605
 | 9.84 | 9.56 | 10.49 | 10.82 | 10.78 | 9.9 | 10.84 | 10.45 | 10.78 | 9.71 | 10.25 | 11.34 | 9.89 | 10.51 | 10.33 | 11.12 | 10.17 | 10.51 | 10.51 | 10.13 | 10.76 | 10.58 | 11.07 | 10.42 | 10.6 | 10.41 | 10.77 | 10.31
 | 10.852 | 11.054 | 10.751 | 11.054 | 11.256 | 10.953 | 10.953 | 10.953 | 10.852 | 10.953 | 10.852 | 10.852 | 11.155 | 11.256 | 11.256 | 11.559 | 11.155 | 11.256 | 11.155 | 11.155 | 10.751 | 10.852 | 11.559 | 11.155 | 10.852 | 11.054 | 10.953 | 11.155
 | 9.752 | 9.954 | 9.651 | 9.954 | 10.156 | 9.853 | 9.853 | 9.853 | 9.752 | 9.853 | 9.752 | 9.752 | 10.055 | 10.156 | 10.156 | 10.459 | 10.055 | 10.156 | 10.055 | 10.055 | 9.651 | 9.752 | 10.459 | 10.055 | 9.752 | 9.954 | 9.853 | 10.055
TS11TSLJ06
TS03TSLJ16
K12TSLJ139
K11TSLJ05
K01TSLJ122
TS05TSLJ12
TS05TSLJ17
TS05TSLJ18
TS12TSLJ01
TS05TSLJ06
TS11TSLJ29
TS03TSLJ25
K03TSLJ13
K03TSLJ23
K01TSLJ112
TS03TSLJ15
TS04TSLJ07
K03TSLJ135
K03TSLJ23
TS04TSLJ19
10.20
K12TSLJ140
TS03TSLJ26
TS03TSLJ11
TS03TSLJ19
TS12TSLJ05
TS11TSLJ27
TSLJ105
TS04TSLJ02
LP(ADB)
TSK(DB)
LP(ADB)+0.55
LP(ADB)-0.55
Location | Method | Ash%
LP | Air Dry basis | 10.40
LP | Dry basis | 10.51
TSK | Dry basis | 10.46
Air Dry (ADB) at LP to Dry Basis (DB) at TSK
Dry basis (DB) at LP to Dry Basis (DB) at TSK
LP(DB)
TSK(DB)
LP(DB)+0.55
LP(DB)-0.55

## Slide 25
Jellinbah PCI reported ash% comparison study w.r.t reporting method March’23-April’24
Chart: 
 | 10.2 | 10.1 | 9.7 | 9.7 | 10.5 | 9.7 | 9.7 | 10.2 | 10.9 | 10.5 | 10.5 | 10.9 | 10.5 | 9.7 | 10.1 | 10.3 | 10.9 | 10.6 | 10.6 | 10.2 | 10.3 | 10.1 | 10.5 | 10.6 | 10.1 | 10.5 | 10.6 | 10.2 | 10.3 | 10.2 | 10.5 | 10.5 | 10.3 | 10.3 | 10.3 | 10.6 | 10.5 | 10.3 | 10.2 | 10.1 | 10.1 | 10.5 | 10.3 | 10.1 | 10.9 | 10.2 | 9.7 | 10.2 | 10.3 | 10.3 | 10.3 | 10.5 | 10.5 | 10.5 | 10.3 | 10.1 | 10.1
 | 9.7 | 10.31 | 11.09 | 10.77 | 11.01 | 10.06 | 11.58 | 11.63 | 11.29 | 11.11 | 10.63 | 10.92 | 10.37 | 10.72 | 10.66 | 10.67 | 11.08 | 11.04 | 11.57 | 10.97 | 10.8 | 10.53 | 10.81 | 11 | 10.97 | 10.79 | 11.14 | 10.87 | 11.04 | 9.23 | 10.84 | 12.3 | 10.77 | 11.48 | 11.43 | 11.73 | 10.87 | 10.89 | 10.69 | 10.87 | 11.25 | 10.56 | 11.22 | 10.96 | 10.87 | 10.6 | 10.57 | 10.63 | 10.77 | 11.8 | 11.06 | 11.11 | 11.02 | 10.38 | 10.89 | 10.8 | 10.56
 | 10.75 | 10.65 | 10.25 | 10.25 | 11.05 | 10.25 | 10.25 | 10.75 | 11.45 | 11.05 | 11.05 | 11.45 | 11.05 | 10.25 | 10.65 | 10.85 | 11.45 | 11.15 | 11.15 | 10.75 | 10.85 | 10.65 | 11.05 | 11.15 | 10.65 | 11.05 | 11.15 | 10.75 | 10.85 | 10.75 | 11.05 | 11.05 | 10.85 | 10.85 | 10.85 | 11.15 | 11.05 | 10.85 | 10.75 | 10.65 | 10.65 | 11.05 | 10.85 | 10.65 | 11.45 | 10.75 | 10.25 | 10.75 | 10.85 | 10.85 | 10.85 | 11.05 | 11.05 | 11.05 | 10.85 | 10.65 | 10.65
 | 9.65 | 9.55 | 9.15 | 9.15 | 9.95 | 9.15 | 9.15 | 9.65 | 10.35 | 9.95 | 9.95 | 10.35 | 9.95 | 9.15 | 9.55 | 9.75 | 10.35 | 10.05 | 10.05 | 9.65 | 9.75 | 9.55 | 9.95 | 10.05 | 9.55 | 9.95 | 10.05 | 9.65 | 9.75 | 9.65 | 9.95 | 9.95 | 9.75 | 9.75 | 9.75 | 10.05 | 9.95 | 9.75 | 9.65 | 9.55 | 9.55 | 9.95 | 9.75 | 9.55 | 10.35 | 9.65 | 9.15 | 9.65 | 9.75 | 9.75 | 9.75 | 9.95 | 9.95 | 9.95 | 9.75 | 9.55 | 9.55
Chart: 
 | 10.302 | 10.201 | 9.797 | 9.797 | 10.605 | 9.797 | 9.797 | 10.302 | 11.009 | 10.605 | 10.605 | 11.009 | 10.605 | 9.797 | 10.201 | 10.403 | 11.009 | 10.706 | 10.706 | 10.302 | 10.403 | 10.201 | 10.605 | 10.706 | 10.201 | 10.605 | 10.706 | 10.302 | 10.403 | 10.302 | 10.605 | 10.605 | 10.403 | 10.403 | 10.403 | 10.706 | 10.605 | 10.403 | 10.302 | 10.201 | 10.201 | 10.605 | 10.403 | 10.201 | 11.009 | 10.302 | 9.797 | 10.302 | 10.403 | 10.403 | 10.403 | 10.605 | 10.605 | 10.605 | 10.403 | 10.201 | 10.201
 | 9.7 | 10.31 | 11.09 | 10.77 | 11.01 | 10.06 | 11.58 | 11.63 | 11.29 | 11.11 | 10.63 | 10.92 | 10.37 | 10.72 | 10.66 | 10.67 | 11.08 | 11.04 | 11.57 | 10.97 | 10.8 | 10.53 | 10.81 | 11 | 10.97 | 10.79 | 11.14 | 10.87 | 11.04 | 9.23 | 10.84 | 12.3 | 10.77 | 11.48 | 11.43 | 11.73 | 10.87 | 10.89 | 10.69 | 10.87 | 11.25 | 10.56 | 11.22 | 10.96 | 10.87 | 10.6 | 10.57 | 10.63 | 10.77 | 11.8 | 11.06 | 11.11 | 11.02 | 10.38 | 10.89 | 10.8 | 10.56
 | 10.852 | 10.751 | 10.347 | 10.347 | 11.155 | 10.347 | 10.347 | 10.852 | 11.559 | 11.155 | 11.155 | 11.559 | 11.155 | 10.347 | 10.751 | 10.953 | 11.559 | 11.256 | 11.256 | 10.852 | 10.953 | 10.751 | 11.155 | 11.256 | 10.751 | 11.155 | 11.256 | 10.852 | 10.953 | 10.852 | 11.155 | 11.155 | 10.953 | 10.953 | 10.953 | 11.256 | 11.155 | 10.953 | 10.852 | 10.751 | 10.751 | 11.155 | 10.953 | 10.751 | 11.559 | 10.852 | 10.347 | 10.852 | 10.953 | 10.953 | 10.953 | 11.155 | 11.155 | 11.155 | 10.953 | 10.751 | 10.751
 | 9.752 | 9.651 | 9.247 | 9.247 | 10.055 | 9.247 | 9.247 | 9.752 | 10.459 | 10.055 | 10.055 | 10.459 | 10.055 | 9.247 | 9.651 | 9.853 | 10.459 | 10.156 | 10.156 | 9.752 | 9.853 | 9.651 | 10.055 | 10.156 | 9.651 | 10.055 | 10.156 | 9.752 | 9.853 | 9.752 | 10.055 | 10.055 | 9.853 | 9.853 | 9.853 | 10.156 | 10.055 | 9.853 | 9.752 | 9.651 | 9.651 | 10.055 | 9.853 | 9.651 | 10.459 | 9.752 | 9.247 | 9.752 | 9.853 | 9.853 | 9.853 | 10.055 | 10.055 | 10.055 | 9.853 | 9.651 | 9.651
K12MBMB161
K02MBMB180
K02MBMB185
K02MBMB193
K02MBMB140
K02MBMB184
K08MBMB127
TS03MBMB06
K03MBMB101
K03MBMB159
TS03MBMB11
K03MBMB156
K02MBMB137
K12MBMB169
MBMB125
TS03MBMB09
K04MBMB128
K03MBMB194
K08MBMB137
MBMB175
K12MBMB171
K03MBMB162
K03MBMB191
K12MBMB156
TS04MBMB02
K03MBMB201
TS12MBMB02
MBMB116
TS11MBMB07
K02MBMB197
K03MBMB168
MBMB107
K04MBMB181
K04MBMB178
K03MBMB205
TS04MBMB08
MBMB122
TS11MBMB11
K12MBMB160
K12MBMB175
TS03MBMB18
K04MBMB177
TS11MBMB04
TS03MBMB07
K08MBMB136
K02MBMB135
TS12MBMB05
MBMB110
K04MBMB183
K12MBMB177
K03MBMB103
K03MBMB164
K03MBMB174
MBMB127
K12MBMB158
K12MBMB165
MBMB133
Location | Method | Ash%
LP | Air Dry basis | 10.30
LP | Dry basis | 10.41
TSM | Dry basis | 10.90
Air Dry(ADB) at LP to Dry Basis(DB) at TSM
LP(ADB)
TSM(DB)
LP(ADB)+0.55
LP(ADB)-0.55
LP(DB)
LP(DB)+0.55
TSM(DB)
LP(DB)-0.55

## Slide 26
MNTH | PORT | RAKE | VESSEL | CONTRACTED | LP(ADB) | TSJ(DB) | TSJ is within ± 0.28 | TSJ is within ± 0.55
28-FEB-2024 | DHM | TS02TWS120 | SAKIZAYA FUTURE | 10.78 | 10 | 10.11 | OK | OK
14-MAR-2023 | DHM | TS03TWS65 | CSK GENERATION | 10.78 | 10.9 | 9.96 | NOT OK | NOT OK
18-JAN-2024 | HLD | T01NHT31 | RGL FIRST | 10.78 | 10.6 | 10.41 | OK | OK
23-MAR-2024 | KICT | K03TWS19 | GRACEOUS | 10.78 | 10.6 | 10.41 | OK | OK
26-FEB-2024 | DHM | TS02TWS108 | SAKIZAYA FUTURE | 10.78 | 10 | 11.04 | NOT OK | NOT OK
27-FEB-2024 | KICT | K02TWS13 | CAPE GENESIS | 10.78 | 10.5 | 10 | NOT OK | OK
21-FEB-2024 | DHM | TS02TWS91 | SAKIZAYA FUTURE | 10.78 | 10 | 10.21 | OK | OK
27-MAR-2024 | KICT | K03TWS24 | GRACEOUS | 10.78 | 10.6 | 10.59 | OK | OK
22-FEB-2024 | DHM | TS02TWS97 | SAKIZAYA FUTURE | 10.78 | 10 | 10.23 | OK | OK
23-MAR-2024 | DHM | TS03TWS74 | ROYAL ARGO | 10.78 | 10.5 | 10.29 | OK | OK
21-AUG-2023 | HLD | T08NHT59 | PELAGIA | 10.78 | 10.2 | 10.59 | NOT OK | OK
10-MAR-2024 | KICT | K03TWS10 | CAPE GENESIS | 10.78 | 10.5 | 10.27 | OK | OK
26-FEB-2024 | DHM | TS02TWS112 | SAKIZAYA FUTURE | 10.78 | 10 | 10 | OK | OK
24-FEB-2024 | DHM | TS02TWS104 | SAKIZAYA FUTURE | 10.78 | 10 | 10.8 | NOT OK | NOT OK
25-MAR-2024 | KICT | K03TWS22 | GRACEOUS | 10.78 | 10.6 | 11.68 | NOT OK | NOT OK
28-FEB-2024 | DHM | TS02TWS116 | SAKIZAYA FUTURE | 10.78 | 10 | 10.02 | OK | OK
20-MAR-2024 | DHM | TS03TWS65 | ROYAL ARGO | 10.78 | 10.5 | 10.18 | NOT OK | OK
02-APR-2023 | DHM | TS04TWS12 | GUO MAY | 10.78 | 10.2 | 8.28 | NOT OK | NOT OK
 |  |  |  |  |  | Rakes(Within tolerance limit) | 10 | 13
 |  |  |  |  |  | Rakes(Outside tolerance limit) | 8 | 5
 |  |  |  |  |  | Total Rakes | 18 | 18
 |  |  |  |  |  | %Rakes(Outside tolerance limit) | 44.44 | 27.78
Jellinbah PCI Coal Ash % reported at TSJ- Comparison of deviation with old vs proposed set point

## Slide 27
Jellinbah PCI Coal Ash % reported at TSK- Comparison of deviation with old vs proposed set point
MNTH | Wagon Type | PORT | RAKE | VESSEL | CONTRACTED | LP(ADB) | TSK(DB) | TSK is within ± 0.28 | TSK is within ± 0.55
09-NOV-2023 | BOXNHL | DHM | TS11TSLJ06 | COLOSSUS | 10.78 | 10.2 | 9.84 | NOT OK | OK
19-MAR-2023 | BOBRN | DHM | TS03TSLJ16 | Cape Olympia | 10.78 | 10.4 | 9.56 | NOT OK | NOT OK
29-DEC-2023 | BOBRN | KICT | K12TSLJ139 | Saiko | 10.78 | 10.1 | 10.49 | OK | OK
22-NOV-2023 | BOXNHL | KICT | K11TSLJ05 | AQUILA OCEAN | 10.78 | 10.4 | 10.82 | OK | OK
14-JAN-2024 | BOBRN | KICT | K01TSLJ122 | RGL FIRST | 10.78 | 10.6 | 10.78 | OK | OK
13-MAY-2023 | BOXN | DHM | TS05TSLJ12 | CHAMPIONSHIP | 10.78 | 10.3 | 9.9 | NOT OK | OK
17-MAY-2023 | BOBRN | DHM | TS05TSLJ17 | CHAMPIONSHIP | 10.78 | 10.3 | 10.84 | OK | OK
18-MAY-2023 | BOXN | DHM | TS05TSLJ18 | CHAMPIONSHIP | 10.78 | 10.3 | 10.45 | OK | OK
01-DEC-2023 | BOBRN | DHM | TS12TSLJ01 | Ubuntu Harmony | 10.78 | 10.2 | 10.78 | OK | OK
06-MAY-2023 | BOBRN | DHM | TS05TSLJ06 | CHAMPIONSHIP | 10.78 | 10.3 | 9.71 | NOT OK | NOT OK
30-NOV-2023 | BOBRN | DHM | TS11TSLJ29 | Ubuntu Harmony | 10.78 | 10.2 | 10.25 | OK | OK
27-MAR-2023 | BOBRN | DHM | TS03TSLJ25 | GUO MAY | 10.78 | 10.2 | 11.34 | OK | OK
12-MAR-2024 | BOXNHL | KICT | K03TSLJ13 | CAPE GENESIS | 10.78 | 10.5 | 9.89 | NOT OK | NOT OK
21-MAR-2024 | BOXNHL | KICT | K03TSLJ23 | GRACEOUS | 10.78 | 10.6 | 10.51 | OK | OK
09-JAN-2024 | BOBRN | KICT | K01TSLJ112 | RGL FIRST | 10.78 | 10.6 | 10.33 | OK | OK
17-MAR-2023 | BOBRN | DHM | TS03TSLJ15 | CSK GENERATION | 10.78 | 10.9 | 11.12 | OK | OK
05-APR-2024 | BOXN | DHM | TS04TSLJ07 | ROYAL ARGO | 10.78 | 10.5 | 10.17 | NOT OK | OK
29-MAR-2024 | BOBRN | KICT | K03TSLJ135 | GRACEOUS | 10.78 | 10.6 | 10.51 | OK | OK
21-MAR-2024 | BOXNHL | KICT | K03TSLJ23 | CAPE GENESIS | 10.78 | 10.5 | 10.51 | OK | OK
18-APR-2024 | BOBRN | DHM | TS04TSLJ19 | ROYAL ARGO | 10.78 | 10.5 | 10.13 | NOT OK | OK
31-DEC-2023 | BOBRN | KICT | K12TSLJ140 | Saiko | 10.78 | 10.1 | 10.76 | OK | OK
28-MAR-2023 | BOBRN | DHM | TS03TSLJ26 | GUO MAY | 10.78 | 10.2 | 10.58 | OK | OK
13-MAR-2023 | BOXNHL | DHM | TS03TSLJ11 | CSK GENERATION | 10.78 | 10.9 | 11.07 | OK | OK
18-MAR-2024 | BOXNHL | DHM | TS03TSLJ19 | ROYAL ARGO | 10.78 | 10.5 | 10.42 | OK | OK
03-DEC-2023 | BOXNHL | DHM | TS12TSLJ05 | Ubuntu Harmony | 10.78 | 10.2 | 10.6 | OK | OK
28-NOV-2023 | BOXNHL | DHM | TS11TSLJ27 | AQUILA OCEAN | 10.78 | 10.4 | 10.41 | OK | OK
04-MAY-2023 | BOBRN | KICT | TSLJ105 | MATISSE | 10.78 | 10.3 | 10.77 | OK | OK
02-APR-2024 | BOBRN | DHM | TS04TSLJ02 | ROYAL ARGO | 10.78 | 10.5 | 10.31 | OK | OK
 |  |  |  |  |  |  | Rakes(Within tolerance limit) | 21 | 25
 |  |  |  |  |  |  | Rakes(Outside tolerance limit) | 7 | 3
 |  |  |  |  |  |  | Total Rakes | 28 | 28
 |  |  |  |  |  |  | %Rakes(Outside tolerance limit) | 25.00 | 10.71

## Slide 28
Jellinbah PCI Coal Ash % reported at TSM- Comparison of deviation with old vs proposed set point
MNTH | Wagon Type | PORT | RAKE | VESSEL | CONTRACTED | LP(ADB) | TSM (DB) | TSM is within ± 0.28 | TSM is within ± 0.55
08-NOV-2023 | BOXNHL | DHM | TS11MBMB04 | COLOSSUS | 10.78 | 10.2 | 9.7 | NOT OK | OK
16-DEC-2023 | BOBRN | KICT | K12MBMB161 | Saiko | 10.78 | 10.1 | 10.31 | OK | OK
23-FEB-2024 | BOBRN | KICT | K02MBMB180 | PACIFIC SARAH | 10.78 | 9.7 | 11.09 | NOT OK | NOT OK
26-FEB-2024 | BOBRN | KICT | K02MBMB185 | PACIFIC SARAH | 10.78 | 9.7 | 10.77 | NOT OK | NOT OK
28-FEB-2024 | BOBRN | KICT | K02MBMB193 | CAPE GENESIS | 10.78 | 10.5 | 11.01 | NOT OK | OK
12-FEB-2024 | BOBRN | KICT | K02MBMB140 | PACIFIC SARAH | 10.78 | 9.7 | 10.06 | NOT OK | OK
24-FEB-2024 | BOBRN | KICT | K02MBMB184 | PACIFIC SARAH | 10.78 | 9.7 | 11.58 | NOT OK | NOT OK
08-AUG-2023 | BOBRN | KICT | K08MBMB127 | PELAGIA | 10.78 | 10.2 | 11.63 | NOT OK | NOT OK
11-MAR-2023 | BOBRN | DHM | TS03MBMB06 | CSK GENERATION | 10.78 | 10.9 | 11.29 | NOT OK | OK
01-MAR-2024 | BOBRN | KICT | K03MBMB101 | CAPE GENESIS | 10.78 | 10.5 | 11.11 | NOT OK | NOT OK
16-MAR-2024 | BOBRN | KICT | K03MBMB159 | CAPE GENESIS | 10.78 | 10.5 | 10.63 | OK | OK
17-MAR-2023 | BOXNS | DHM | TS03MBMB11 | CSK GENERATION | 10.78 | 10.9 | 10.92 | OK | OK
16-MAR-2024 | BOBRN | KICT | K03MBMB156 | CAPE GENESIS | 10.78 | 10.5 | 10.37 | OK | OK
12-FEB-2024 | BOBRN | KICT | K02MBMB137 | PACIFIC SARAH | 10.78 | 9.7 | 10.72 | NOT OK | NOT OK
18-DEC-2023 | BOBRN | KICT | K12MBMB169 | Saiko | 10.78 | 10.1 | 10.66 | NOT OK | NOT OK
08-MAY-2023 | BOBRN | KICT | MBMB125 | MATISSE | 10.78 | 10.3 | 10.67 | NOT OK | OK
15-MAR-2023 | BOXNHL | DHM | TS03MBMB09 | CSK GENERATION | 10.78 | 10.9 | 11.08 | OK | OK
11-APR-2024 | BOBRN | KICT | K04MBMB128 | GRACEOUS | 10.78 | 10.6 | 11.04 | NOT OK | OK
26-MAR-2024 | BOBRN | KICT | K03MBMB194 | GRACEOUS | 10.78 | 10.6 | 11.57 | NOT OK | NOT OK
11-AUG-2023 | BOBRN | KICT | K08MBMB137 | PELAGIA | 10.78 | 10.2 | 10.97 | NOT OK | NOT OK
22-MAY-2023 | BOBRN | KICT | MBMB175 | MATISSE | 10.78 | 10.3 | 10.8 | NOT OK | OK
18-DEC-2023 | BOBRN | KICT | K12MBMB171 | Saiko | 10.78 | 10.1 | 10.53 | NOT OK | OK
18-MAR-2024 | BOBRN | KICT | K03MBMB162 | CAPE GENESIS | 10.78 | 10.5 | 10.81 | NOT OK | OK
25-MAR-2024 | BOBRN | KICT | K03MBMB191 | GRACEOUS | 10.78 | 10.6 | 11 | NOT OK | OK
15-DEC-2023 | BOBRN | KICT | K12MBMB156 | Saiko | 10.78 | 10.1 | 10.97 | NOT OK | NOT OK
09-APR-2024 | BOXNHL | DHM | TS04MBMB02 | ROYAL ARGO | 10.78 | 10.5 | 10.79 | NOT OK | OK
27-MAR-2024 | BOBRN | KICT | K03MBMB201 | GRACEOUS | 10.78 | 10.6 | 11.14 | NOT OK | OK
02-DEC-2023 | BOXNHL | DHM | TS12MBMB02 | Ubuntu Harmony | 10.78 | 10.2 | 10.87 | NOT OK | NOT OK
06-MAY-2023 | BOBRN | KICT | MBMB116 | MATISSE | 10.78 | 10.3 | 11.04 | NOT OK | NOT OK
16-NOV-2023 | BOBRN | DHM | TS11MBMB07 | Ubuntu Harmony | 10.78 | 10.2 | 9.23 | NOT OK | NOT OK
28-FEB-2024 | BOBRN | KICT | K02MBMB197 | CAPE GENESIS | 10.78 | 10.5 | 10.84 | NOT OK | OK
19-MAR-2024 | BOBRN | KICT | K03MBMB168 | CAPE GENESIS | 10.78 | 10.5 | 12.3 | NOT OK | NOT OK
03-MAY-2023 | BOBRN | KICT | MBMB107 | MATISSE | 10.78 | 10.3 | 10.77 | NOT OK | OK
24-APR-2024 | BOBRN | KICT | K04MBMB181 | NEFELI.GR | 10.78 | 10.3 | 11.48 | NOT OK | NOT OK

## Slide 29
Jellinbah PCI Coal Ash % reported at TSM- Comparison of deviation with old vs proposed set point
MNTH | Wagon Type | PORT | RAKE | VESSEL | CONTRACTED | LP(ADB) | TSM (DB) | TSM is within ± 0.28 | TSM is within ± 0.55
24-APR-2024 | BOBRN | KICT | K04MBMB178 | NEFELI.GR | 10.78 | 10.3 | 11.43 | NOT OK | NOT OK
28-MAR-2024 | BOBRN | KICT | K03MBMB205 | GRACEOUS | 10.78 | 10.6 | 11.73 | NOT OK | NOT OK
23-APR-2024 | BOBRN | DHM | TS04MBMB08 | ROYAL ARGO | 10.78 | 10.5 | 10.87 | NOT OK | OK
07-MAY-2023 | BOBRN | KICT | MBMB122 | MATISSE | 10.78 | 10.3 | 10.89 | NOT OK | NOT OK
28-NOV-2023 | BOXN | DHM | TS11MBMB11 | Ubuntu Harmony | 10.78 | 10.2 | 10.69 | NOT OK | OK
16-DEC-2023 | BOBRN | KICT | K12MBMB160 | Saiko | 10.78 | 10.1 | 10.87 | NOT OK | NOT OK
19-DEC-2023 | BOBRN | KICT | K12MBMB175 | Saiko | 10.78 | 10.1 | 11.25 | NOT OK | NOT OK
31-MAR-2024 | BOXN | DHM | TS03MBMB18 | ROYAL ARGO | 10.78 | 10.5 | 10.56 | OK | OK
23-APR-2024 | BOBRN | KICT | K04MBMB177 | NEFELI.GR | 10.78 | 10.3 | 11.22 | NOT OK | NOT OK
20-DEC-2023 | BOBRN | KICT | K12MBMB177 | Saiko | 10.78 | 10.1 | 10.96 | NOT OK | NOT OK
13-MAR-2023 | BOXN | DHM | TS03MBMB07 | CSK GENERATION | 10.78 | 10.9 | 10.87 | OK | OK
11-AUG-2023 | BOBRN | KICT | K08MBMB136 | PELAGIA | 10.78 | 10.2 | 10.6 | NOT OK | OK
11-FEB-2024 | BOBRN | KICT | K02MBMB135 | PACIFIC SARAH | 10.78 | 9.7 | 10.57 | NOT OK | NOT OK
08-DEC-2023 | BOXNHL | DHM | TS12MBMB05 | Ubuntu Harmony | 10.78 | 10.2 | 10.63 | NOT OK | OK
04-MAY-2023 | BOBRN | KICT | MBMB110 | MATISSE | 10.78 | 10.3 | 10.77 | NOT OK | OK
25-APR-2024 | BOBRN | KICT | K04MBMB183 | NEFELI.GR | 10.78 | 10.3 | 11.8 | NOT OK | NOT OK
10-MAY-2023 | BOBRN | KICT | MBMB133 | MATISSE | 10.78 | 10.3 | 11.06 | NOT OK | NOT OK
02-MAR-2024 | BOBRN | KICT | K03MBMB103 | CAPE GENESIS | 10.78 | 10.5 | 11.11 | NOT OK | NOT OK
18-MAR-2024 | BOBRN | KICT | K03MBMB164 | CAPE GENESIS | 10.78 | 10.5 | 11.02 | NOT OK | OK
20-MAR-2024 | BOBRN | KICT | K03MBMB174 | CAPE GENESIS | 10.78 | 10.5 | 10.38 | OK | OK
08-MAY-2023 | BOBRN | KICT | MBMB127 | MATISSE | 10.78 | 10.3 | 10.89 | NOT OK | NOT OK
16-DEC-2023 | BOBRN | KICT | K12MBMB158 | Saiko | 10.78 | 10.1 | 10.8 | NOT OK | NOT OK
17-DEC-2023 | BOBRN | KICT | K12MBMB165 | Saiko | 10.78 | 10.1 | 10.56 | NOT OK | OK
 |  |  |  |  |  |  | Rakes(Within tolerance limit) | 8 | 29
 |  |  |  |  |  |  | Rakes(Outside tolerance limit) | 49 | 28
 |  |  |  |  |  |  | Total Rakes | 57 | 57
 |  |  |  |  |  |  | %Rakes(Outside tolerance limit) | 85.96 | 49.12

## Slide 30
Jellinbah PCI Coal Ash % reported at TSJ- Comparison of deviation w.r.t method of reporting
MNTH | PORT | RAKE | VESSEL | LP(ADB) | LP(DB) | TSJ(DB) | TSJ is within +-0.28(ADB-DB) | TSJ is within +-0.28(DB-DB)
28-FEB-2024 | DHM | TS02TWS120 | SAKIZAYA FUTURE | 10 | 10.10 | 10.11 | OK | OK
14-MAR-2023 | DHM | TS03TWS65 | CSK GENERATION | 10.9 | 11.01 | 9.96 | NOT OK | NOT OK
18-JAN-2024 | HLD | T01NHT31 | RGL FIRST | 10.6 | 10.71 | 10.41 | OK | NOT OK
23-MAR-2024 | KICT | K03TWS19 | GRACEOUS | 10.6 | 10.71 | 10.41 | OK | NOT OK
26-FEB-2024 | DHM | TS02TWS108 | SAKIZAYA FUTURE | 10 | 10.10 | 11.04 | NOT OK | NOT OK
27-FEB-2024 | KICT | K02TWS13 | CAPE GENESIS | 10.5 | 10.61 | 10 | NOT OK | NOT OK
21-FEB-2024 | DHM | TS02TWS91 | SAKIZAYA FUTURE | 10 | 10.10 | 10.21 | OK | OK
27-MAR-2024 | KICT | K03TWS24 | GRACEOUS | 10.6 | 10.71 | 10.59 | OK | OK
22-FEB-2024 | DHM | TS02TWS97 | SAKIZAYA FUTURE | 10 | 10.10 | 10.23 | OK | OK
23-MAR-2024 | DHM | TS03TWS74 | ROYAL ARGO | 10.5 | 10.61 | 10.29 | OK | NOT OK
21-AUG-2023 | HLD | T08NHT59 | PELAGIA | 10.2 | 10.30 | 10.59 | NOT OK | NOT OK
10-MAR-2024 | KICT | K03TWS10 | CAPE GENESIS | 10.5 | 10.61 | 10.27 | OK | NOT OK
26-FEB-2024 | DHM | TS02TWS112 | SAKIZAYA FUTURE | 10 | 10.10 | 10 | OK | OK
24-FEB-2024 | DHM | TS02TWS104 | SAKIZAYA FUTURE | 10 | 10.10 | 10.8 | NOT OK | NOT OK
25-MAR-2024 | KICT | K03TWS22 | GRACEOUS | 10.6 | 10.71 | 11.68 | NOT OK | NOT OK
28-FEB-2024 | DHM | TS02TWS116 | SAKIZAYA FUTURE | 10 | 10.10 | 10.02 | OK | OK
20-MAR-2024 | DHM | TS03TWS65 | ROYAL ARGO | 10.5 | 10.61 | 10.18 | NOT OK | NOT OK
02-APR-2023 | DHM | TS04TWS12 | GUO MAY | 10.2 | 10.30 | 8.28 | NOT OK | NOT OK
 |  |  |  |  |  | Rakes(Within tolerance limit) | 10 | 6
 |  |  |  |  |  | Rakes(Outside tolerance limit) | 8 | 12
 |  |  |  |  |  | Total Rakes | 18 | 18
 |  |  |  |  |  | %Rakes(Outside tolerance limit) | 44.44 | 66.67

## Slide 31
Jellinbah PCI Coal Ash % reported at TSK- Comparison of deviation w.r.t method of reporting
MNTH | Wagon Type | PORT | RAKE | VESSEL | LP(ADB) | LP(DB) | TSK(DB) | TSK is within +-0.28(ADB-DB) | TSK is within +-0.28(DB-DB)
09-NOV-2023 | BOXNHL | DHM | TS11TSLJ06 | COLOSSUS | 10.2 | 10.30 | 9.84 | NOT OK | NOT OK
19-MAR-2023 | BOBRN | DHM | TS03TSLJ16 | Cape Olympia | 10.4 | 10.50 | 9.56 | NOT OK | NOT OK
29-DEC-2023 | BOBRN | KICT | K12TSLJ139 | Saiko | 10.1 | 10.20 | 10.49 | OK | OK
22-NOV-2023 | BOXNHL | KICT | K11TSLJ05 | AQUILA OCEAN | 10.4 | 10.50 | 10.82 | OK | OK
14-JAN-2024 | BOBRN | KICT | K01TSLJ122 | RGL FIRST | 10.6 | 10.71 | 10.78 | OK | OK
13-MAY-2023 | BOXN | DHM | TS05TSLJ12 | CHAMPIONSHIP | 10.3 | 10.40 | 9.9 | NOT OK | NOT OK
17-MAY-2023 | BOBRN | DHM | TS05TSLJ17 | CHAMPIONSHIP | 10.3 | 10.40 | 10.84 | OK | OK
18-MAY-2023 | BOXN | DHM | TS05TSLJ18 | CHAMPIONSHIP | 10.3 | 10.40 | 10.45 | OK | OK
01-DEC-2023 | BOBRN | DHM | TS12TSLJ01 | Ubuntu Harmony | 10.2 | 10.30 | 10.78 | OK | OK
06-MAY-2023 | BOBRN | DHM | TS05TSLJ06 | CHAMPIONSHIP | 10.3 | 10.40 | 9.71 | NOT OK | NOT OK
30-NOV-2023 | BOBRN | DHM | TS11TSLJ29 | Ubuntu Harmony | 10.2 | 10.30 | 10.25 | OK | OK
27-MAR-2023 | BOBRN | DHM | TS03TSLJ25 | GUO MAY | 10.2 | 10.30 | 11.34 | OK | OK
12-MAR-2024 | BOXNHL | KICT | K03TSLJ13 | CAPE GENESIS | 10.5 | 10.61 | 9.89 | NOT OK | NOT OK
21-MAR-2024 | BOXNHL | KICT | K03TSLJ23 | GRACEOUS | 10.6 | 10.71 | 10.51 | OK | OK
09-JAN-2024 | BOBRN | KICT | K01TSLJ112 | RGL FIRST | 10.6 | 10.71 | 10.33 | OK | NOT OK
17-MAR-2023 | BOBRN | DHM | TS03TSLJ15 | CSK GENERATION | 10.9 | 11.01 | 11.12 | OK | OK
05-APR-2024 | BOXN | DHM | TS04TSLJ07 | ROYAL ARGO | 10.5 | 10.61 | 10.17 | NOT OK | NOT OK
29-MAR-2024 | BOBRN | KICT | K03TSLJ135 | GRACEOUS | 10.6 | 10.71 | 10.51 | OK | OK
21-MAR-2024 | BOXNHL | KICT | K03TSLJ23 | CAPE GENESIS | 10.5 | 10.61 | 10.51 | OK | OK
18-APR-2024 | BOBRN | DHM | TS04TSLJ19 | ROYAL ARGO | 10.5 | 10.61 | 10.13 | NOT OK | NOT OK
31-DEC-2023 | BOBRN | KICT | K12TSLJ140 | Saiko | 10.1 | 10.20 | 10.76 | OK | OK
28-MAR-2023 | BOBRN | DHM | TS03TSLJ26 | GUO MAY | 10.2 | 10.30 | 10.58 | OK | OK
13-MAR-2023 | BOXNHL | DHM | TS03TSLJ11 | CSK GENERATION | 10.9 | 11.01 | 11.07 | OK | OK
18-MAR-2024 | BOXNHL | DHM | TS03TSLJ19 | ROYAL ARGO | 10.5 | 10.61 | 10.42 | OK | OK
03-DEC-2023 | BOXNHL | DHM | TS12TSLJ05 | Ubuntu Harmony | 10.2 | 10.30 | 10.6 | OK | OK
28-NOV-2023 | BOXNHL | DHM | TS11TSLJ27 | AQUILA OCEAN | 10.4 | 10.50 | 10.41 | OK | OK
04-MAY-2023 | BOBRN | KICT | TSLJ105 | MATISSE | 10.3 | 10.40 | 10.77 | OK | OK
02-APR-2024 | BOBRN | DHM | TS04TSLJ02 | ROYAL ARGO | 10.5 | 10.61 | 10.31 | OK | NOT OK
 |  |  |  |  |  |  | Rakes(Within tolerance limit) | 21 | 19
 |  |  |  |  |  |  | Rakes(Outside tolerance limit) | 7 | 9
 |  |  |  |  |  |  | Total Rakes | 28 | 28
 |  |  |  |  |  |  | %Rakes(Outside tolerance limit) | 25.00 | 32.14

## Slide 32
Jellinbah PCI Coal Ash % reported at TSM- Comparison of deviation w.r.t method of reporting
MNTH | PORT | RAKE | VESSEL | CONTRACTED | LP(ADB) | LP(DB) | TSM(DB) | TSM is within +-0.28(ADB-DB) | TSM is within +-0.28(DB-DB)
08-NOV-2023 | DHM | TS11MBMB04 | COLOSSUS | 10.78 | 10.2 | 10.30 | 9.7 | NOT OK | NOT OK
16-DEC-2023 | KICT | K12MBMB161 | Saiko | 10.78 | 10.1 | 10.20 | 10.31 | OK | OK
23-FEB-2024 | KICT | K02MBMB180 | PACIFIC SARAH | 10.78 | 9.7 | 9.80 | 11.09 | NOT OK | NOT OK
26-FEB-2024 | KICT | K02MBMB185 | PACIFIC SARAH | 10.78 | 9.7 | 9.80 | 10.77 | NOT OK | NOT OK
28-FEB-2024 | KICT | K02MBMB193 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 11.01 | NOT OK | NOT OK
12-FEB-2024 | KICT | K02MBMB140 | PACIFIC SARAH | 10.78 | 9.7 | 9.80 | 10.06 | NOT OK | OK
24-FEB-2024 | KICT | K02MBMB184 | PACIFIC SARAH | 10.78 | 9.7 | 9.80 | 11.58 | NOT OK | NOT OK
08-AUG-2023 | KICT | K08MBMB127 | PELAGIA | 10.78 | 10.2 | 10.30 | 11.63 | NOT OK | NOT OK
11-MAR-2023 | DHM | TS03MBMB06 | CSK GENERATION | 10.78 | 10.9 | 11.01 | 11.29 | NOT OK | NOT OK
01-MAR-2024 | KICT | K03MBMB101 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 11.11 | NOT OK | NOT OK
16-MAR-2024 | KICT | K03MBMB159 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 10.63 | OK | OK
17-MAR-2023 | DHM | TS03MBMB11 | CSK GENERATION | 10.78 | 10.9 | 11.01 | 10.92 | OK | OK
16-MAR-2024 | KICT | K03MBMB156 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 10.37 | OK | OK
12-FEB-2024 | KICT | K02MBMB137 | PACIFIC SARAH | 10.78 | 9.7 | 9.80 | 10.72 | NOT OK | NOT OK
18-DEC-2023 | KICT | K12MBMB169 | Saiko | 10.78 | 10.1 | 10.20 | 10.66 | NOT OK | NOT OK
08-MAY-2023 | KICT | MBMB125 | MATISSE | 10.78 | 10.3 | 10.40 | 10.67 | NOT OK | OK
15-MAR-2023 | DHM | TS03MBMB09 | CSK GENERATION | 10.78 | 10.9 | 11.01 | 11.08 | OK | OK
11-APR-2024 | KICT | K04MBMB128 | GRACEOUS | 10.78 | 10.6 | 10.71 | 11.04 | NOT OK | NOT OK
26-MAR-2024 | KICT | K03MBMB194 | GRACEOUS | 10.78 | 10.6 | 10.71 | 11.57 | NOT OK | NOT OK
11-AUG-2023 | KICT | K08MBMB137 | PELAGIA | 10.78 | 10.2 | 10.30 | 10.97 | NOT OK | NOT OK
22-MAY-2023 | KICT | MBMB175 | MATISSE | 10.78 | 10.3 | 10.40 | 10.8 | NOT OK | NOT OK
18-DEC-2023 | KICT | K12MBMB171 | Saiko | 10.78 | 10.1 | 10.20 | 10.53 | NOT OK | NOT OK
18-MAR-2024 | KICT | K03MBMB162 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 10.81 | NOT OK | OK
25-MAR-2024 | KICT | K03MBMB191 | GRACEOUS | 10.78 | 10.6 | 10.71 | 11 | NOT OK | NOT OK
15-DEC-2023 | KICT | K12MBMB156 | Saiko | 10.78 | 10.1 | 10.20 | 10.97 | NOT OK | NOT OK
09-APR-2024 | DHM | TS04MBMB02 | ROYAL ARGO | 10.78 | 10.5 | 10.61 | 10.79 | NOT OK | OK
27-MAR-2024 | KICT | K03MBMB201 | GRACEOUS | 10.78 | 10.6 | 10.71 | 11.14 | NOT OK | NOT OK
02-DEC-2023 | DHM | TS12MBMB02 | Ubuntu Harmony | 10.78 | 10.2 | 10.30 | 10.87 | NOT OK | NOT OK
06-MAY-2023 | KICT | MBMB116 | MATISSE | 10.78 | 10.3 | 10.40 | 11.04 | NOT OK | NOT OK

## Slide 33
Jellinbah PCI Coal Ash % reported at TSM- Comparison of deviation w.r.t method of reporting
MNTH | PORT | RAKE | VESSEL | CONTRACTED | LP(ADB) | LP(DB) | TSM(DB) | TSM is within +-0.28(ADB-DB) | TSM is within +-0.28(DB-DB)
16-NOV-2023 | DHM | TS11MBMB07 | Ubuntu Harmony | 10.78 | 10.2 | 10.30 | 9.23 | NOT OK | NOT OK
28-FEB-2024 | KICT | K02MBMB197 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 10.84 | NOT OK | OK
19-MAR-2024 | KICT | K03MBMB168 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 12.3 | NOT OK | NOT OK
03-MAY-2023 | KICT | MBMB107 | MATISSE | 10.78 | 10.3 | 10.40 | 10.77 | NOT OK | NOT OK
24-APR-2024 | KICT | K04MBMB181 | NEFELI.GR | 10.78 | 10.3 | 10.40 | 11.48 | NOT OK | NOT OK
24-APR-2024 | KICT | K04MBMB178 | NEFELI.GR | 10.78 | 10.3 | 10.40 | 11.43 | NOT OK | NOT OK
28-MAR-2024 | KICT | K03MBMB205 | GRACEOUS | 10.78 | 10.6 | 10.71 | 11.73 | NOT OK | NOT OK
23-APR-2024 | DHM | TS04MBMB08 | ROYAL ARGO | 10.78 | 10.5 | 10.61 | 10.87 | NOT OK | OK
07-MAY-2023 | KICT | MBMB122 | MATISSE | 10.78 | 10.3 | 10.40 | 10.89 | NOT OK | NOT OK
28-NOV-2023 | DHM | TS11MBMB11 | Ubuntu Harmony | 10.78 | 10.2 | 10.30 | 10.69 | NOT OK | NOT OK
16-DEC-2023 | KICT | K12MBMB160 | Saiko | 10.78 | 10.1 | 10.20 | 10.87 | NOT OK | NOT OK
19-DEC-2023 | KICT | K12MBMB175 | Saiko | 10.78 | 10.1 | 10.20 | 11.25 | NOT OK | NOT OK
31-MAR-2024 | DHM | TS03MBMB18 | ROYAL ARGO | 10.78 | 10.5 | 10.61 | 10.56 | OK | OK
23-APR-2024 | KICT | K04MBMB177 | NEFELI.GR | 10.78 | 10.3 | 10.40 | 11.22 | NOT OK | NOT OK
20-DEC-2023 | KICT | K12MBMB177 | Saiko | 10.78 | 10.1 | 10.20 | 10.96 | NOT OK | NOT OK
13-MAR-2023 | DHM | TS03MBMB07 | CSK GENERATION | 10.78 | 10.9 | 11.01 | 10.87 | OK | OK
11-AUG-2023 | KICT | K08MBMB136 | PELAGIA | 10.78 | 10.2 | 10.30 | 10.6 | NOT OK | NOT OK
11-FEB-2024 | KICT | K02MBMB135 | PACIFIC SARAH | 10.78 | 9.7 | 9.80 | 10.57 | NOT OK | NOT OK
08-DEC-2023 | DHM | TS12MBMB05 | Ubuntu Harmony | 10.78 | 10.2 | 10.30 | 10.63 | NOT OK | NOT OK
04-MAY-2023 | KICT | MBMB110 | MATISSE | 10.78 | 10.3 | 10.40 | 10.77 | NOT OK | NOT OK
25-APR-2024 | KICT | K04MBMB183 | NEFELI.GR | 10.78 | 10.3 | 10.40 | 11.8 | NOT OK | NOT OK
10-MAY-2023 | KICT | MBMB133 | MATISSE | 10.78 | 10.3 | 10.40 | 11.06 | NOT OK | NOT OK
02-MAR-2024 | KICT | K03MBMB103 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 11.11 | NOT OK | NOT OK
18-MAR-2024 | KICT | K03MBMB164 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 11.02 | NOT OK | NOT OK
20-MAR-2024 | KICT | K03MBMB174 | CAPE GENESIS | 10.78 | 10.5 | 10.61 | 10.38 | OK | OK
08-MAY-2023 | KICT | MBMB127 | MATISSE | 10.78 | 10.3 | 10.40 | 10.89 | NOT OK | NOT OK
16-DEC-2023 | KICT | K12MBMB158 | Saiko | 10.78 | 10.1 | 10.20 | 10.8 | NOT OK | NOT OK
17-DEC-2023 | KICT | K12MBMB165 | Saiko | 10.78 | 10.1 | 10.20 | 10.56 | NOT OK | NOT OK
 |  |  |  |  |  |  | Rakes(Within tolerance limit) | 8 | 14
 |  |  |  |  |  |  | Rakes(Outside tolerance limit) | 49 | 43
 |  |  |  |  |  |  | Total Rakes | 57 | 57
 |  |  |  |  |  |  | %Rakes(Outside tolerance limit) | 85.96 | 75.44

## Slide 34
Set points for Coal Ash % precision as per IS 16143
V1 =3 for ash contents for washed coals
= 0.20
S.No | Description | TSJ | TSK
V1 | Primary Increment Variance | 3 | 3
VPT | Preparation and testing variance | 0.2 | 0.2
n | No of increments per sub lots | 12 | 40
m | No of sublots in the lot | 6 | 1
PL | Overall precision of sampling , sample preparation and testing for the lot | 0.55 | 1.05
 | Frequency of increment collection | 5-7 min | 3 min
 | Belt Speed | 1000 tph | 1800tph

## Slide 35
 |  | TSJ | TSK | EXP
V1 | Primary Increment Variance | 3 | 3 | 3
VPT | Preparation and testing variance | 0.2 | 0.2 | 0.05
n | No of increments per sub lots | 12 | 40 | 20
m | No of sublots in the lot | 6 | 1 | 8
PL | Overall precision of sampling , sample preparation and testing for the lot | 0.55 | 1.05 | 0.32
 | Frequency of increment collection | 5-7 min | 3 min | NA
 | Belt Speed | 1000 tph | 1800tph | NA
Set points for Coal Ash % precision as per IS 16143 for plant sites